The prospect of a green laser

based on AlGaN/AlN structures heavily doped with silicon

P.A. Bokhan, N.V. Fateev, T.V. Malin, Dm.E. Zakrevsky, K.S. Zhuravlev

Rzhanov Institute of Semiconductor Physics SB RAS, Novosibirsk 630090, Russia

The AlxGa1-xN alloys with a bandgap in the range of 3.4–6.2 eV has emerged as perspective semiconductor materials with applications to laser sources. Luminescent properties of the AlxGa1-xN films with Si dopant concentration more than 1020 cm-3 grown by molecular beam epitaxy on sapphire substrates with AlN buffer film were investigate. Time-resolved photoluminescence spectroscopy was employed to study the donor-acceptor pair transitions in the AlxGa1-xN/AlN/Al2O3 structures with Al mole fraction x from 0.56 to 1 under action of Nd:YAG laser radiation with λ = 266 nm (4.66 eV).

The radiation inside planar waveguide consists of spontaneous emission and amplified spontaneous emission. The spontaneous emission spectra demonstrated inhomogeneous broadening with FWHM of 0.51 eV covers full visible range and propagate randomly in all directions. The measured values of quantum yield of spontaneous luminescence are ~ 0.8, 0.5, 0.14 for Al0.74Ga0.26N, Al0.65Ga0.35N and Al0.5Ga0.5N films, respectively.

The amplified spontaneous emission propagates at near the critical angle of incidence along zigzag path under total internal reflection conditions at the interfaces of the waveguide. Its spectrum consists of several TEm and TMm modes, which have mutually orthogonal polarizations. The optical measured gains are equals to g ≈ 58 cm-1 for Al0.65Ga0.35N at 510 nm and g ≈ 20 cm-1 for Al0.74Ga0.26N films at λ = 528 nm, applying the stripe excitation method under optical pumping. The decay curves of the amplified spontaneous emission from the films after action of pumping radiation is described by the sum of two exponential dependences with characteristic time as τf (the fast decay time) and τs (the slow decay time). Experimental results shows that the τf decreases as a function of the pump power density. When the pump power density is reduced to zero, then τf approaches the spontaneous decay time τs, which are differ for the various structures. Decay times τs for Al0.74Ga0.26N and Al0.65Ga0.35N films are equals to 90 ns and 40 ns respectively. The estimated emission cross-sections  are 1.5×10-18 and 3.1×10-18 cm2 for the Al0.74Ga0.26N and Al0.65Ga0.35N structures respectively. Using the values for the optical gain values, we find the population inversion ΔN ≈ 1.3×1019 cm-3 for Al0.74Ga0.26N and ΔN ≈ 1.9×1019 cm-3 for Al0.65Ga0.35N films.

To obtain amplifying medium for light waves, the possible four level scheme for creating population inverse in AlGaN films was considered.